Sunline Technical Fabrics

EIFS FIBERGLASS MESH SPECIFICATIONS

SELF EXTINGUISHING    E=GLASS

| Fabric Weight | Fabric Weave | Roll Width | Roll Length | Area Covered |
| --- | --- | --- | --- | --- |
| 4.5 Oz/Sq Yd | Leno 6 x 6 | 38” | 150 Ft | 475 Sq Ft |

| Fabric Weight Before Coating | Aperture Size | Thickness | Coating | Resin Content of Coating |
| --- | --- | --- | --- | --- |
| 3.8 Oz/Sq Yd | 0.14” x 0.14” | .019” | Modified Acrylic | 15% |

| Average Tensile Warp/Weft | Retained Tensile* Warp/Weft | Elongation Warp/Weft | #### Alkali* Resistant |
| --- | --- | --- | --- |
| > 200 Lbs/Inch | > 120 Lbs/Inch | 4.5 | Yes |

#### EIMA Standard 105.01 – ASTM E 2098-00 #### Standard Test Method for Alkali Resistance of Glass Fiber Reinforcing Mesh #### for Use in Exterior Insulation and Finish System (EIFS), Class PB

*After 28 Day Immersion in a 5% (NaOH) Solution Average Retention Rate for Tensile Strength > 120 Lbs/Inch Test Results Confirmed By Specialized Technology Resources ISO 9002

| #### Packaging |  |  |  |  |
| --- | --- | --- | --- | --- |
| 4 Rolls/Carton | 9 Cartons/Pallet (36 Rolls) | Rolls Covered In Plastic | 16.5 Lbs/Roll | 660 Lbs/Pallet |