Sunline Technical Fabrics

EIFS FIBERGLASS MESH SPECIFICATIONS

SELF EXTINGUISHING    E=GLASS

| Fabric Weight | Fabric Weave | Roll Width | Roll Length | Area Covered |
| --- | --- | --- | --- | --- |
| 4.3 Oz/Sq Yd | Leno 4 x 4 | 38” | 150 Ft | 475 Sq Ft |

| Fabric Weight Before Coating | Coating | Alkali Resistant | Resin Content of Coating |
| --- | --- | --- | --- |
| 3.6 Oz/Sq Yd | Modified Acrylic | Yes | 18-20% |

#### EIMA Standard 105.01 – ASTM E 2098-00 #### Standard Test Method for Alkali Resistance of Glass Fiber Reinforcing Mesh #### for Use in Exterior Insulation and Finish System (EIFS), Class PB

*After 28 Day Immersion in a 5% (NaOH) Solution Average Retention Rate for Tensile Strength > 120 Lbs/70%

| #### Packaging |  |  |  |  |
| --- | --- | --- | --- | --- |
| 4 Rolls/Carton | 9 Cartons/Pallet (36 Rolls) | Rolls Covered In Plastic | 16.5 Lbs/Roll | 660 Lbs/Pallet |